## Slide 1: CMOS VLSI Design Lecture 5: Nonideal Transistor Theory
Notes: Hello and welcome. Today, in the CMOS VLSI Design, our focus will be on Nonideal transistor theory.

## Slide 2: Learning Objectives
At the end of this lecture, you should be able to:
Use suitable equations to describe the nonideal transistor characteristics due to High field effects, Channel length modulation, Threshold voltage effects and Leakage.
Explain sources and impacts of process and environmental variations on the transistor operation.
Notes: By the end of this lecture, you should be able to
Use suitable equations to describe the nonideal transistor characteristics due to High field effects, Channel length modulation, Threshold voltage effects and Leakage.
Explain sources and impacts of process and environmental variations on the transistor operation.

## Slide 3: Outline
Nonideal Transistor Behavior
  High Field Effects
    Mobility Degradation
    Velocity Saturation
  Channel Length Modulation
  Threshold Voltage Effects
    Body Effect
    Drain-Induced Barrier Lowering
    Short Channel Effect
  Leakage
    Subthreshold Leakage
    Gate Leakage
    Junction Leakage
Process and Environmental Variations

## Slide 4: Ideal Transistor I-V
Shockley long-channel transistor models

## Slide 5: Ideal vs. Simulated nMOS I-V Plot
65 nm IBM process, VDD = 1.0 V
Notes: Plot shows Simulated vs Ideal I-V characteristics of the nMOS transistor. This plot highlights the difference between the ideal and non-ideal transistor. In the plot, it can be seen that the velocity saturation and mobility degradation for the simulated model is lower than that of the ideal transistor.

## Slide 6: ON and OFF Current
Ion = Ids @ Vgs = Vds = VDD
  Saturation
Ioff = Ids @ Vgs = 0, Vds = VDD
  Cutoff
Notes: For the transistor to operate in saturation, the following conditions have to be met: Vgs = Vds = VDD.
For the transistor to operate in cutoff, the following conditions have to be met: Vgs = 0, Vds = VDD.

## Slide 7: Electric Fields Effects
Vertical electric field: Evert = Vgs / tox
  Attracts carriers into channel
  Long channel: Qchannel proportional to Evert
Lateral electric field: Elat = Vds / L
  Accelerates carriers from drain to source
  Long channel: v = µElat
Notes: There are two different types of electric field effects for our transistors.
The first one is the vertical electrical field, which is equal to:
Voltage from gate to source over the gate oxide thickness. This field attracts carriers into the channel. In long channel MOSFETs the charge in the channel is proportional to the vertical electric field.
The second electric field is the lateral one which is equal to:
Voltage from drain to source over the space between them. This field accelerates carriers from drain to source. In long channel MOSFETs v = µElat.

## Slide 8: Coffee Cart Analogy
Tired student runs from VLSI lab to coffee cart
Freshmen are pouring out of the physics lecture hall
Vds is how long you have been up
  Your velocity = fatigue × mobility
Vgs is a wind blowing you against the glass (SiO2) wall
At high Vgs, you are buffeted against the wall
  Mobility degradation
At high Vds, you scatter off freshmen, fall down, get up
  Velocity saturation
    Don’t confuse this with the saturation region

## Slide 9: Mobility Degradation
High Evert effectively reduces mobility
  Collisions with oxide interface
Notes: A high vertical electric field effectively reduces mobility because there are more collisions with the oxide interface.
Equation to calculate μ eff for either n or p transistors.

## Slide 10: Velocity Saturation
At high Elat, carrier velocity rolls off
  Carriers scatter off atoms in silicon lattice
  Velocity reaches vsat
    Electrons: 107 cm/s
    Holes: 8 x 106 cm/s
  Better model

## Slide 11: Vel Sat I-V Effects
Ideal transistor ON current increases with VDD2
Velocity-saturated ON current increases with VDD
Real transistors are partially velocity saturated
  Approximate with α-power law model
  Ids scales with VDDα
  1 < α < 2 determined empirically (≈ 1.3 for 65 nm)

## Slide 12: a-Power Model
Notes: The α-Power model is used to determine the drain-current for short channel MOSFETs.
The α-Power model is based on four parameters: Vth (threshold voltage), α (velocity saturation index), Vdsat (drain saturation voltage) and ldsat (drain current).
The concept behind the α-Power model for short-channel MOSFETs is that the drain current of is proportional to .
With the α-power model, the curves are more linear as the value of α changes, which could be between 1 and 2.
The α-Power model is used to determine the drain-current for short channel MOSFETs.
The α-Power model is based on four parameters: Vth (threshold voltage), α (velocity saturation index), Vdsat (drain saturation voltage) and ldsat (drain current).
The concept behind the α-Power model for short-channel MOSFETs is that the drain current of is proportional to 〖"(Vgs − Vth )" 〗^"α" .
With the α-power model, the curves are more linear as the value of α changes, which could be between 1 and 2.

## Slide 13: Channel Length Modulation
Reverse-biased p-n junctions form a depletion region
  Region between n and p with no carriers
  Width of depletion, Ld, region grows with reverse bias
  Leff = L – Ld
Shorter Leff gives more current
  Ids increases with Vds
  Even in saturation
Notes: A channel length modulation is a shortening of the length of the inverted channel.
Reverse-biased p-n junctions form a depletion region with no carriers, and the width of depletion region grows with reverse bias so that the effective channel length is equal to total channel length minus width of depletion.
A shorter effect channel length gives more current and Ids increases with Vds.

## Slide 14: Chan Length Mod I-V
λ = channel length modulation coefficient
  not feature size
  Empirically fit to I-V characteristics
Notes: Channel length modulation or CML can be represented by current and voltage.
We can calculate the drain source current with following formula where lambda is equal to the channel length modulation coefficients.

## Slide 15: Threshold Voltage Effects
Vt is Vgs for which the channel starts to invert
Ideal models assumed Vt is constant
Really depends (weakly) on almost everything else:
  Body voltage: Body Effect
  Drain voltage: Drain-Induced Barrier Lowering
  Channel length: Short Channel Effect
Notes: Threshold voltage is equal to gate source voltage for which the channel starts to invert. Ideal models assumed that threshold voltage is constant.
It really depends (weakly) on almost everything else, like:
Body voltage: Body effect
Drain voltage: Drain-Induced Barrier Lowering
And Channel length: Short Channel Effect
Next, we will examine how these affect the threshold voltage.

## Slide 16: Body Effect
Body is a fourth transistor terminal
Vsb affects the charge required to invert the channel
  Increasing Vs or decreasing Vb increases Vt
Vt0 = nominal threshold voltage
fs = surface potential at threshold
  Depends on doping level NA
  And intrinsic carrier concentration ni
g = body effect coefficient
Notes: The body is the fourth transistor terminal.
Source to body voltage affects the charge required to invert the channel. Thus, when the source voltage is increased or the body voltage is decreased, the threshold voltage increases.

## Slide 17: Body Effect Cont.
For small source-to-body voltage, treat as linear
Notes: For a small source to body voltage, the formula to calculate the threshold is treated as linear.

## Slide 18: DIBL
Electric field from drain affects channel
More pronounced in small transistors where the drain is closer to the channel
Drain-Induced Barrier Lowering
  Drain voltage also affect Vt
High drain voltage causes current to increase.
Notes: Electric fields due to drain voltage affect the channel. This is more pronounced in small transistors where drain is closer to the channel. This effect is called the Drain-Induced barrier lowering or DIBL (the drain voltage affects the threshold voltage).
A high drain voltage causes current Ids to increase when the transistor is operating in saturation region.
We can model the effect of DIBL on the threshold voltage with the formula shown in the slide where Eta(η) is the DIBL coefficient.

## Slide 19: Short Channel Effect
In small transistors, source/drain depletion regions extend into the channel
  Impacts the amount of charge required to invert the channel
  And thus makes Vt a function of channel length
Short channel effect: Vt increases with L
  Some processes exhibit a reverse short channel effect in which Vt decreases with L
Notes: In small transistors, the source/drain depletion region extends into a significant part of the channel. This could increase the amount of charge required to create an inversion region between the source and drain. Thus Vt becomes a function of the channel length.
Some processes exhibit a reverse short channel effect in which Vt decreases with L.

## Slide 20: Leakage
What about current in cutoff?
Simulated results
What differs?
  Current doesn’t
  go to 0 in cutoff
Notes: Leakage can occur when a transistor is OFF.
In the simulated model, the current doesn’t go to zero in the cutoff region.

## Slide 21: Leakage Sources
Subthreshold conduction
  Transistors can’t abruptly turn ON or OFF
  Dominant source in contemporary transistors
Gate leakage
  Tunneling through ultrathin gate dielectric
Junction leakage
  Reverse-biased PN junction diode current
Notes: There are different types of leakage sources, such as:
Subthreshold conduction makes transistor unable to abruptly turn ON or OFF; this leakage source is dominant in the contemporary transistors.
Gate leakage caused by tunneling through the gate dielectric due to being extremely thin.
Junction leakage: here current flows through the reverse biased p-n junction between the source/drain and the body.

## Slide 22: Subthreshold Leakage
Subthreshold leakage exponential with Vgs
n is process dependent
  typically 1.3-1.7
Rewrite relative to Ioff on log scale
S ≈ 100 mV/decade @ room temperature
Notes: When the gate falls below Vt , i.e Vgs < Vt weak inversion occurs. In this state, the subthreshold leakage current increases with Vds because of DIBL.
In the equation, Ids0 is dependent on process and device geometry. This is the current at threshold.
n is a process-dependent term typically ranges from 1.3–1.7 for CMOS processes and is affected by the depletion region characteristics.

## Slide 23: Gate Leakage
Carriers tunnel through very thin gate oxides
Exponentially sensitive to tox and VDD
  A and B are tech constants
  Greater for electrons
    So nMOS gates leak more
Negligible for older processes (tox > 20 Å)
Critically important at 65 nm and below (tox ≈ 10.5 Å)
From [Song01]
Notes: Gate leakage can be due to direct tunneling in which carriers tunnel through very thin gate oxides resulting in leakage current through the gate.
Gate leakage is sensitive to the thickness of the gate oxide and it increases as the oxide thickness is reduced.
You can calculate the current leakage with the formula below, where a and b are physical parameters, which can become greater for electrons, so nMOS gates leak more.
This leakage is important at 65 nanometers and below because the thickness of gates is approximately 10.5 angstrom.

## Slide 24: Junction Leakage
Reverse-biased p-n junctions have some leakage
  Ordinary diode leakage
  Band-to-band tunneling (BTBT)
  Gate-induced drain leakage (GIDL)
Notes: In the diagram, the p-n junction is shown between:
Source/drain diffusions and substrate/ well.
n well – p substrate .
reverse-biased p-n junctions have some leakage like the ordinary diode leakage, band-to-band tunneling or BTBT, and gate-induced drain leakage (GIDL).

## Slide 25: Diode Leakage
Reverse-biased p-n junctions have some leakage
At any significant negative diode voltage, ID = -Is
Is depends on doping levels
  And area and perimeter of diffusion regions
  Typically <1 fA/µm2 (negligible)
Notes: The n well – p substrate junction is reversed biased. However, small current ID can still flow through this junction.
In the case of the diode leakage, we can calculate its current with the formula given.
A significantly reversed biased junction (negative diode voltage) more than the thermal voltage, the leakage current ID = –IS,
IS depends on doping levels and area and perimeter of diffusion regions and is negligible.

## Slide 26: Band-to-Band Tunneling
Tunneling across heavily doped p-n junctions
  Especially sidewall between drain & channel
  when halo doping is used to increase Vt
Increases junction leakage to significant levels
  Xj: sidewall junction depth
  Eg: bandgap voltage
  A, B: tech constants
Notes: Band-to-Band Tunneling affects heavily doped drains. BTBT occurs on the p-n junctions formed between the drain/source and the body when reversed biased. High halo doping is used to increase Vt, however, this instead causes BTBT to grow.
Leakage due to BTBT can be modeled with the formula shown in the slide.

## Slide 27: Gate-Induced Drain Leakage
Occurs at overlap between gate and drain
  Most pronounced when drain is at VDD, gate is at a negative voltage
  Thwarts efforts to reduce subthreshold leakage using a negative gate voltage
Notes: Gate-induced drain leakage occurs at overlap between gate and drain.
This leakage is the most pronounced when the drain is at Vdd/high voltage and the gate is at negative/low.

## Slide 28: Temperature Sensitivity
Increasing temperature
  Reduces mobility
  Reduces Vt
ION decreases with temperature
IOFF increases with temperature
Notes: Transistors are temperature sensitive, increasing its temperature can reduce its mobility and its threshold voltage.
When transistor is ON, the current decreases with temperature.
When transistor is OFF, its current increases with temperature.

## Slide 29: So What?
So what if transistors are not ideal?
  They still behave like switches.
But these effects matter for…
  Supply voltage choice
  Logical effort
  Quiescent power consumption
  Pass transistors
  Temperature of operation

## Slide 30: Parameter Variation
Transistors have uncertainty in parameters
  Process: Leff, Vt, tox of nMOS and pMOS
  Vary around typical (T) values
Fast (F)
  Leff: short
  Vt: low
  tox: thin
Slow (S): opposite
Not all parameters are independent
for nMOS and pMOS
Notes: Transistors have uncertainty in parameters such as Process (effective channel length, threshold voltage, or thickness of gate oxide of nMOS and pMOS) These parameters vary around typical (T) values.
The parameters for a fast transistor are short effective channel length, low threshold voltage and thin thickness of the gate oxide. The opposite will give a slow transistor.

## Slide 31: Environmental Variation
VDD and T also vary in time and space
Fast:
  VDD: high
  T: low
Corner | Voltage | Temperature
F | 1.98 | 0 C
T | 1.8 | 70 C
S | 1.62 | 125 C
Notes: There is also a variation because of the environment. Sources of environmental variation are Vdd and temperature.

## Slide 32: Process Corners
Process corners describe worst case variations
  If a design works in all corners, it will probably work for any variation.
Describe corner with four letters (T, F, S)
  nMOS speed
  pMOS speed
  Voltage
  Temperature
Notes: Process corners describe worst case variation that helps us to know whether a design will work for any variation of the corners.
The corners are described with four letters, T for typical, F for fast, and S for slow. And these are assigned to each of the parameter of our transistor as:
nMOS or pMOS speed, voltage, and temperature.

## Slide 33: Important Corners
Some critical simulation corners include
Purpose | nMOS | pMOS | VDD | Temp
Cycle time | S | S | S | S
Power | F | F | F | F
Subthreshold leakage | F | F | F | S